# Inspection Report IR-2026-7101 - Vessel V-7101

Unit: CDU-7 Crude Distillation. Equipment: V-7101 Overhead Accumulator. Service: Class-A hydrocarbon. Design pressure 21.0 barg. Design temperature 165 degC.

Nominal shell thickness 14.0 mm. Corrosion allowance 3.0 mm. Minimum allowable thickness t-min 11.0 mm per API 510.

# Ultrasonic thickness survey

| Location | Survey 15-Mar-2021 (mm) | Survey 15-Mar-2026 (mm) |
| --- | --- | --- |
| Shell Course-1 | 13.1 | 11.6 |
| Shell Course-2 | 13.4 | 12.7 |
| Shell Course-3 | 13.6 | 13.2 |
| Head - top | 13.9 | 13.6 |

Course-1 is the governing location. The interval between the two surveys is exactly 5.0 years.

Inspector: M. Rao, API 510 cert 41882. Next external inspection due 15-Mar-2028.

NOTE: Heat exchanger E-7204 was scheduled for thickness survey in this campaign but the survey was NOT carried out - scaffolding was unavailable. No thickness data exists for E-7204 in this report or any other.