# Vessel Thickness Survey - V-3302

Unit: Unit 33 - Diesel Hydrodesulphuriser (DHDS). Equipment: V-3302 HP Separator.

# 1. Equipment particulars

| Field | Value |
| --- | --- |
| Design Pressure | 62.0 barg |
| Design Temperature | 370 degC |
| Material | SA-387 Gr.11 |
| Year of Manufacture | 2009 |
| Nominal Shell Thickness | 22.00 mm |
| Corrosion Allowance | 3.00 mm |
| Minimum Required Thickness (t-min) | 15.50 mm |
| Inspection Code | API 510 |

# 2. Ultrasonic thickness readings - shell course 1

All readings in millimetres. Same CML grid used on both surveys.

| CML | Survey A (06-Apr-2023) | Survey B (06-Apr-2027) |
| --- | --- | --- |
| CML-01 | 20.10 | 19.02 |
| CML-02 | 19.85 | 18.61 |
| CML-03 | 19.40 | 18.20 |
| CML-04 | 18.60 | 16.60 |
| CML-05 | 19.95 | 18.95 |
| CML-06 | 20.40 | 19.60 |

# 3. Remarks

Governing (thinnest) location is CML-04 on both surveys. The interval between Survey A and Survey B is exactly 4.000 years. No repair, weld overlay or re-rating was carried out between the two surveys. Corrosion rate and remaining life have deliberately NOT been calculated in this report.

Inspector: S. Bhatt, API 510 #47720