# Shell Thickness Survey - E-3304

Unit: Unit 33 - Diesel Hydrodesulphuriser (DHDS). Equipment: E-3304 Reactor Feed / Effluent Exchanger, shell side.

| Field | Value |
| --- | --- |
| Code minimum thickness (t-min) | 9.20 mm |
| Measured, governing CML-03 | 8.75 mm |
| Survey date | 10-Apr-2027 |

The measured thickness is below the code t-min by 0.45 mm. Refer to the Inspection Section before returning to service.