# MRPL — EQUIPMENT INSPECTION REPORT

Report No: MRPL/INSP/2026/0412    Unit: CDU-II    Date: 12-Sep-2026

# 1. Equipment Particulars

| Tag No | Description | Design Pressure | Last Inspected |
| --- | --- | --- | --- |
| TK-4102 | Crude Storage Tank | Atmospheric | 14-Mar-2024 |
| PSV-2041 | Safety Relief Valve | 12.5 barg | 14-Mar-2024 |
| P-4110A | Crude Transfer Pump | 18.0 barg | 02-Aug-2025 |

# 2. Observations

a) Shell plate thickness at course-1 measured 11.2 mm against nominal 12.0 mm. Loss of 0.8 mm over 24 months.

b) PSV-2041 set pressure found at 12.5 barg; SOP-114 specifies 14.0 barg. Deviation not previously documented.

c) Minor external corrosion observed near nozzle N-3. No through-wall loss.

d) Foundation grouting intact. No settlement recorded.

# 3. Recommendation

Re-rate TK-4102 per API 653 or restore thickness at next shutdown. PSV-2041 to be bench-tested and reset to 14.0 barg before restart.

Inspected by: R. Nair (API 510 #48112)    Reviewed by: S. Kulkarni