# EQUIPMENT INSPECTION REPORT

Unit: U-1000    Date: 12-Sep-2026    Inspector: R. Nair

# 1. Equipment

| Tag | Description | Nominal (mm) | Measured (mm) |
| --- | --- | --- | --- |
| T-1001 | Crude Feed Tank | 20.0 | 18.4 |
| E-1001 | Preheat Exchanger | 14.0 | 13.1 |

# 2. Observations

T-1001 measured 18.4 mm against nominal 20.0 mm over 40 months. Minimum required 17.2 mm.

E-1001 measured 13.1 mm against nominal 14.0 mm over 40 months.

E-1002 was not surveyed during this campaign.

PSV-1001 as-found 26.0 barg.