# EQUIPMENT INSPECTION REPORT

Unit: U-500    Date: 12-Sep-2026    Inspector: R. Nair

# 1. Equipment

| Tag | Description | Nominal (mm) | Measured (mm) |
| --- | --- | --- | --- |
| T-501 | Surge Drum | 16.0 | 14.2 |
| P-501 | Distribution Pump | 15.0 | 14.6 |
| E-501 | Trim Cooler | 13.0 | 11.9 |

# 2. Observations

T-501 course-1 measured 14.2 mm against nominal 16.0 mm over 45 months. Minimum required 12.4 mm.

E-501 shell measured 11.9 mm against nominal 13.0 mm over 30 months. Minimum required 11.2 mm.

PSV-501 as-found 14.8 barg.

PSV-502 as-found 6.2 barg.

LT-501 indicates 78 percent level at survey.