# EQUIPMENT INSPECTION REPORT

Unit: SET-6    Date: 12-Sep-2026    Inspector: R. Nair

# 1. Equipment

| Tag | Description | Nominal (mm) | Measured (mm) |
| --- | --- | --- | --- |
| V-601 | Feed Drum | 15.0 | 13.1 |
| R-601 | Reactor | 20.0 | 19.2 |

# 2. Observations

V-601 course-1 measured 13.1 mm against nominal 15.0 mm over 38 months. Minimum required 12.6 mm.

PSV-601 as-found 17.5 barg.

PT-601 reads 16.9 barg at normal operation.