# EQUIPMENT INSPECTION REPORT

Unit: SET-1    Date: 12-Sep-2026    Inspector: R. Nair

# 1. Equipment

| Tag | Description | Nominal (mm) | Measured (mm) |
| --- | --- | --- | --- |
| V-101 | Storage Drum | 10.0 | 9.4 |
| PSV-101 | Relief Valve | - | - |

# 2. Observations

Shell thickness at course-1 measured 9.4 mm against nominal 10.0 mm. Interval since last survey: 24 months.

PSV-101 as-found set pressure 9.0 barg. SOP-201 requires 10.0 barg.

Minimum required thickness per API 653 calculation: 8.6 mm.