# EQUIPMENT INSPECTION REPORT

Unit: SET-4    Date: 12-Sep-2026    Inspector: R. Nair

# 1. Equipment

| Tag | Description | Nominal (mm) | Measured (mm) |
| --- | --- | --- | --- |
| E-401 | Shell & Tube Exchanger | 18.0 | 16.2 |
| V-401 | Knock-out Drum | 11.0 | 10.6 |

# 2. Observations

E-401 shell measured 16.2 mm against nominal 18.0 mm over 48 months. Minimum required 15.0 mm.

V-401 shell measured 10.6 mm against nominal 11.0 mm over 24 months. Minimum required 9.8 mm.

TI-401 outlet temperature 168 degC.

PSV-401 as-found 7.4 barg.