MANGALORE REFINERY AND PETROCHEMICALS LIMITED

# EXCHANGER SHELL THICKNESS SURVEY - E-2404

| Document No. | NHT-INSP-2026-033 |
| --- | --- |
| Revision | 0 |
| Date | 12-Mar-2026 |
| Unit | Unit 24 - Naphtha Hydrotreater |
| Tag Number | E-2404 |
| Service | Feed / Reactor Effluent Exchanger, shell side |
| Material | SA-516 Gr. 70 |
| Design Pressure (shell) | 21.0 barg |
| Nominal Shell Thickness | 12.00 mm |
| Minimum Required Thickness (t-min) | 8.50 mm |

## Ultrasonic Thickness Readings

| CML Point | Reading 12-Mar-2026 (mm) | Status vs t-min 8.50 mm |
| --- | --- | --- |
| CML-01 | 9.40 | Above t-min |
| CML-02 | 8.85 | Above t-min |
| CML-03 | 8.20 | BELOW t-min |
| CML-04 | 9.05 | Above t-min |
| CML-05 | 8.61 | Above t-min |
| MINIMUM | 8.20 | BELOW t-min |

## Remarks

Governing location CML-03 reads 8.20 mm against a minimum required thickness of 8.50 mm. This is a shortfall of 0.30 mm below the code minimum and is reported here as an apparent non-conformance.

The Inspection Engineer is to check whether any approved deviation is in force for this exchanger before initiating a repair or replacement recommendation. This report does not itself clear or condemn the item.

Surveyed by: A. Bhandary, ASNT Level II UT (Cert. 4471)

Reviewed by: S. Nayak, Inspection Engineer